# Manufacturing Processes

Consolidated Lecture Notes: Casting, Pattern Making, and Welding Processes

Compiled from Lectures 2–12

# Contents

- Lecture 2 – Pattern and Allowances

- Lecture 3 – Moulding Sand

- Lecture 4 – Molding and Core Making

- Lecture 5 – Gating System

- Lecture 6 – Die Casting and Centrifugal Casting

- Lecture 7 – Investment Casting

- Lecture 8 – Welding: Concept and Classification

- Lecture 9 – Gas Welding and Types of Flame

- Lecture 10 – Electric Arc Welding: SMAW and Submerged Arc Welding

- Lecture 11 – Resistance Welding

- Lecture 12 – Soldering and Brazing

# Lecture 2 – Pattern and Allowances

## Casting

Casting is the process of producing metallic parts by pouring molten metal into the mould and allowing the metal to solidify.

## Casting Process (sequence of steps)

- Mould is prepared

- Metal is heated above melting point temperature

- Liquid metal is poured into the mould

- Metal solidifies into the shape of the mould

- Casted part is removed from the mould

- Post-casting operations: Cutting, Clean up, Machining

## Pattern

A pattern is a replica of a casting to be made. Using a pattern, impressions (mould cavity) can be formed in the damp sand to make a mould.

### Pattern Materials

- Wood: easy to work and readily available; can be cut into required shapes; used when a small number of castings are needed

- Metal: does not change shape when subjected to moist conditions; used for a small number of castings

- Plastics: do not absorb moisture; smooth; can be withdrawn from the mould easily without damaging the mould

- Plaster: high compressive strength

### Types of Patterns

- Single piece pattern

- Match plate pattern

- Gated pattern

- Split pattern

- Cope & Drag pattern

- Loose-piece pattern

- Skeleton pattern

### Description of Pattern Types

- Single piece pattern: made from one piece and does not contain loose pieces; inexpensive and of the simplest type

- Split pattern: most widely used pattern for intricate castings; the pattern is split into two parts so that one part is in the cope and the other in the drag; the two halves are aligned properly using dowel pins

- Cope and Drag pattern: similar to split patterns; the cope and drag halves of the pattern, along with the gating and riser systems, are prepared separately and attached to the metal or wooden plate along with alignment pins

- Match plate pattern: an extension of the cope and drag pattern; the cope and drag patterns, along with the gating and risering, are mounted on a single matching (metal) plate on either side

- Loose piece pattern: used when the contour of the part is such that withdrawing the pattern from the mould is not possible; the obstructing part is held as a loose piece

- Skeleton pattern: made of strips of wood for preparing the final pattern by pouring sand around the pattern and packing it

- Gated pattern: usually made of metal, which increases strength and reduces tendency to warp; the section connecting different patterns serves as runner and gates; a gated pattern can manufacture many castings at one time; used in mass production systems

Figure: Types of patterns

## Complete Mould Assembly (Cross-Section)

Figure: Green sand mould with pattern — first operation, second operation, and complete mould

## Pattern Allowances

- Shrinkage allowance

- Draft or Taper allowance

- Machining or Finishing allowance

- Camber or Distortion allowance

- Shake or Rapping allowance

### 1. Shrinkage Allowance

- Most metals used in casting contract during cooling from pouring temperature to room temperature

- Provided to compensate for solid contraction by providing adequate allowance in the pattern

- Amount of contraction varies with different metals

Figure: Shrinkage allowance

### 2. Machining Allowance

- Given on the surface of the pattern by increasing the metal thickness there, to compensate for loss of metal due to machining on these surfaces

- Depends mainly on the method of machining to be employed

- Given in addition to the shrinkage allowance

Figure: Machining allowance

### 3. Draft or Taper Allowance

- A slight taper is given on the vertical surfaces of the pattern, parallel to the direction of withdrawal from the mould

- Provided on both internal and external surfaces

- For easy withdrawal of the pattern from the mould

Figure: Draft/taper allowance — without draft vs with draft

### 4. Rapping (Shake) Allowance

- A negative allowance to be provided in the pattern

- When the pattern is withdrawn from the mould by striking (rapping) it from side to side, the size of the cavity increases

- To compensate for this, rapping allowance is provided

### 5. Distortion Allowance

- Castings having an irregular shape will not have uniform contraction during cooling, resulting in distortion of the casting

- Remedy: an opposite distortion is provided in the pattern

Figure: Cooling behaviour and distortion allowance (camber)

# Lecture 3 – Moulding Sand

## Classification of Moulding Sand

- Natural moulding sand (Green sand): taken from river-beds and contains a major amount of clay; easily available at low cost

- Synthetic sand: contains little or no binder (clay); strength and bonding property can be easily controlled; more expensive than natural sand

- Special sand: ideal for obtaining special characteristics

### Types of Moulding Sand (by use)

- Green Sand: contains silica sand, clay, and water; possesses good strength and permeability

- Dry Sand: stronger and more thermally stable than green sand; used for larger, heavier castings

- Loam Sand: a mixture with high clay content (around 50%); used for large castings with skeleton patterns

- Facing Sand: used to form the mould face, providing a smooth surface for the casting and preventing metal penetration

- Backing Sand: supports the facing sand and fills the rest of the mould cavity; contains permeability

- System Sand: applied in machine moulding; possesses high strength, permeability, and refractoriness

- Core Sand: used to make cores; includes binders such as linseed oil, phenol-formaldehyde, urea-formaldehyde, dextrin, starch, sodium silicate, and fire clay

- Parting Sand: used to prevent sand from sticking together at the parting line of the mould

## Sand Preparation

- Very few natural sands have all the qualities required by a moulding sand

- It is mixed with other sands that possess the required characteristics

- Sufficient moisture must be added to the sand

- Sand must be properly conditioned before use

## Properties of a Moulding Sand

- Porosity (Permeability): sand must be porous to allow gases/moisture present within the mould to be removed freely when molten metal is poured

- Adhesiveness: sand particles must be capable of adhering to the sides of moulding boxes

- Cohesiveness / Strength: ability of sand particles to stick together; must be sufficient to permit the mould to be formed to the desired shape even after hot metal is poured in

- Refractoriness: moulding sands with poor refractoriness may burn onto the casting; measured by the sinter point of sand

- Collapsibility: mould made of sand should collapse as the molten metal solidifies in it

- Flowability: ability of the sand to behave like a fluid so that, when rammed, sand flows to all portions of the mould and around the pattern, taking up the required shape; increases as clay and water content increase; high flowability is required for uniform density and a good impression of the pattern

## Key Components of Sand

- Silica Sand: the base material of the mould (typically silica sand)

- Clay: binds the sand particles together, providing strength and durability to the mould (e.g., bentonite, kaolinite)

- Water: essential for the binding properties of clay in green sand

- Binders (Resins): used in dry sand or resin sand casting to create a strong, solid mould, e.g., phenolic resins, furan resins, urea resins, epoxy resins, acrylic resins

- Auxiliary Substances: may include sawdust, coal powder, or straw, improving air permeability and heat resistance of the mould

### Typical Composition Ranges

- Silica sand (SiO2): primary mould material, provides refractoriness; typical range 80–92%

- Clay: acts as a binder; common types include bentonite clay (e.g., sodium bentonite); typical range 6–12%

- Water: activates the clay binder, enabling it to hold sand grains together; typical range 3–6%

- Other additives: include sea coal, silica flour, and other organic materials; improve flowability, permeability of the mould, and surface finish of the casting

## Green Sand Mould – Key Parts (as illustrated)

- Drag, Cope, Pattern, Molding board

- Vents, Lifter, Weight

- Pouring basin, Sprue pin, Riser pin, Riser

- Parting line, Runner, Gate, Core

## Molding Tools

Figure: Common moulding tools — shovel, riddle, trowel, vent wire, strike-off bar, bellow, draw spike, mallet, lifter, slick, swab

Reference video link provided in lecture: https://www.youtube.com/watch?v=FihNxujyu08

# Lecture 4 – Molding and Core Making

## Conventional Molding Process: Green Sand Molding

Green sand is the most diversified molding method used in metal casting operations. The process utilizes a mould made of compressed or compacted moist sand. The term "green" denotes the presence of moisture in the molding sand. The mould material consists of silica sand mixed with a suitable bonding agent (usually clay) and moisture.

### Advantages

- Most metals can be cast by this method

- Pattern costs and material costs are relatively low

- No limitation with respect to size of casting and type of metal or alloy used

### Disadvantages

- Surface finish of the castings obtained by this process is not good; machining is often required to achieve the finished product

## Green Sand Molding Steps

- The first step is to place the pattern on the molding board

- The drag is placed on the board

- Dry facing sand is sprinkled over the board and pattern to provide a non-sticky layer

- Molding sand is riddled in to cover the pattern with the fingers; then the drag is completely filled

- The sand is firmly packed in the drag by means of hand rammers; ramming must be proper — neither too hard nor too soft

- After ramming, excess sand is leveled off with a straight bar known as a strike-off bar

- With the help of a vent rod, vent holes are made in the drag to facilitate removal of gases during pouring and solidification

- The finished drag flask is rolled over to the bottom board, exposing the pattern

- The cope half of the pattern is placed over the drag pattern with the help of locating pins; the cope flask on the drag is located, aligning again with pins

- Dry parting sand is sprinkled all over the drag and on the pattern

- A sprue pin for making the sprue passage is located at a small distance from the pattern; a riser pin, if required, is also placed at an appropriate place

- Filling, ramming, and venting of the cope proceed in the same manner as performed in the drag

- The sprue and riser pins are removed first, and a pouring basin is scooped out at the top to pour the liquid metal

- The pattern from the cope and drag is removed; facing sand in the form of paste is applied, if required, all over the mould cavity and runners to give the finished casting a good surface finish

- The mould is now assembled and ready for pouring

## Core

A core is a specialized insert, typically made of sand, that creates hollow spaces or intricate internal features within a cast part. Cores are used to form internal cavities, recesses, undercuts, and other features in castings that the mould itself cannot create. Cores are crucial for producing a wide variety of cast components, from engine blocks with internal cooling passages to more complex shapes with internal features.

## Core Making Steps

- Selection of Sand: properties of core sand are highly crucial and required to have characteristics like permeability, green strength, refractoriness, flowability, collapsibility, adhesiveness, cohesiveness, and dry strength

- Mixing of sand with additives: after thorough mixing of sand, binder is added to the silica sand with moisture content and other additives like coal dust, dextrin, or silica flour to create a mixture

- Blowing or Shooting: mixture is blown into the core box (core shooting process); modern foundries use dedicated core blowing/shooting machines for optimal production

- Venting: essential to provide a venting passage for gases, as trapped gases can result in casting defects; additional venting holes are made in cores to obtain good permeability

- Reinforcement of Cores: heavy and large cores in particular might need additional reinforcement material like cast iron grids or low-carbon steel wires to maintain coherence

- Baking of Cores: to obtain strength, baking of sand cores is done in a conventional oven at temperature between 200°C to 250°C (392°F to 482°F); the heat causes the binder to polymerize

- Cleaning & Finishing: after baking — Trimming (removing loose pieces and unwanted projections), Brushing (removes loose sand off the core with a fine wire brush), Coating (crucial step for finishing; coating cores with refractory material to improve heat resistance)

- Inspection: manual or machine inspection of cores for dimensional accuracy

- Assembling: assembling of multiple cores together with core glue and placement of core in mould

Figure: Mould without core vs mould with core (assembled core)

# Lecture 5 – Gating System

## Gating System

A gate is a specific part of the gating system, acting as the entry point for molten metal into the mould cavity. It is designed to control the flow rate and direction of the molten metal as it enters the mould. Gates can be designed in various shapes and sizes, depending on the casting process, material, and desired part characteristics. The gate's design and placement are crucial for achieving a sound and defect-free casting.

## Requirements of Gating System

- A good gating design should ensure proper distribution of molten metal without excessive temperature loss, turbulence, gas entrapment, and slags

- Slow pouring increases filling time, leading to premature solidification; hence super heating of metal is required, but this may cause solubility issues

- Faster pouring of molten metal causes erosion of the mould cavity

- Gating design is important and depends on the metal and molten metal composition — for example, aluminium can get oxidized easily

## Functions of Gating System

- Controlling flow: gates regulate the rate at which molten metal enters the mould cavity, preventing turbulence and ensuring smooth, consistent flow

- Minimizing defects: by controlling flow, gates help prevent issues like air entrapment, shrinkage, and porosity

- Directing metal flow: gates can be strategically placed to guide molten metal to specific areas of the mould, ensuring proper filling of complex shapes

- Shrinkage control: in some cases, gates are designed to act as risers, providing a reservoir of molten metal to compensate for shrinkage during solidification

## Aspiration Effect

Aspiration effect: entering of gases from baking of organic compounds present in the mould into the molten metal stream, producing porous castings. Pressure anywhere in the liquid stream should not become negative.

## Types of Gates

- Top Gate: molten metal enters the mould cavity from the top; simple but can cause turbulence and erosion

- Bottom Gate: molten metal enters the mould cavity from the bottom; can lead to temperature variations within the casting, with the bottom being hotter and the top cooler

- Parting Line Gate: molten metal enters the mould cavity at the parting line, where the two halves of the mould meet; simple and cost-effective, but prone to erosion and dross formation

- Step Gate: used in the sand casting process for producing heavy castings of large size; used when the molten metal requirement is large and metal needs to fill the mould cavity in steps

## Gating System Parts

Figure: Gating system parts — pouring basin/cup, sprue, sprue well, runner, gate, riser

- Pouring Basin: a funnel-shaped reservoir at the top of the mould (sprue hole) where molten metal is initially poured from the crucible

- Sprue: the vertical channel that connects the pouring basin to the runner system and controls the flow rate of the metal

- Sprue Well: a small reservoir at the bottom of the sprue, which regulates the flow of metal into the runner and reduces turbulence

- Runner: the horizontal channel(s) that distribute molten metal from the sprue to the gates

- Runner Extension: an elongated part of the runner, used to feed multiple gates or as a collection place for impurities

- In-gate (or Gate): end opening through which molten metal enters the mould cavity

## Riser

- Riser acts as a metal reservoir which holds extra molten metal, ensuring flow of metal into the mould cavity as the casting material shrinks

- Riser should be the last part of the mould to solidify, ensuring continuous feeding of metal until the complete casting has solidified

- Provides shrinkage compensation of molten metal, without which shrinkage would create voids or porosity within the casting

- Prevents defects by preventing shrinkage cavities and maintaining the desired shape and dimensions

# Lecture 6 – Die Casting and Centrifugal Casting

## Hot Chamber Die Casting

- Good for low temperature metals (approx. 650°C)

- Faster than cold chamber machines

- Cycle times must be short to minimize metal contamination

- Metal starts in a heated cylinder

- A piston forces metal into the die

- The piston retracts and draws metal in

- Metals used: Lead, Tin, Zinc

Figure: Hot chamber die casting machine

## Cold Chamber Die Casting

- Casts high melting point metals (> 700°C)

- High pressures used

- Metal is heated in a separate crucible

- Metal is ladled into a cold chamber

- The metal is rapidly forced into the mould before it cools

- Copper, Brass, and Aluminum can be cast

Figure: Cold chamber die casting machine

### Characteristics of Cold Chamber Die Casting

- Extremely smooth surfaces (1 µm)

- Excellent dimensional accuracy

- Rapid production rate

- Better mechanical properties compared to sand casting

- Intricate parts possible

### Summary Table: Hot Chamber vs Cold Chamber Die Casting

| Parameter | Hot Chamber | Cold Chamber |
| --- | --- | --- |
| Materials | Zinc, Magnesium | Aluminum, Copper, Brass |
| Pressure Range | 7–40 MPa | 20–150 MPa |
| Metal Feeding | Integrated (gooseneck) | Manual ladling |
| Cycle Time | Faster | Slower |
| Melting Temp | Low | High |

## Die Casting – General Points

- High initial die cost

- Limited to high-fluidity nonferrous metals

- Part size is limited

- Porosity may be a problem

- Some scrap in sprues, runners, and flash, but this can be directly recycled

### Applications

- Carburetors

- Automotive parts

- Bathroom fixtures

- Toys

### Common Metals

Alloys of aluminum, zinc, magnesium, and lead. Also possible with alloys of copper and tin.

## Centrifugal Casting

Centrifugal casting is a metal casting process that utilizes centrifugal force to distribute molten metal into a rotating mould, producing cylindrical or symmetrical parts. This method is particularly effective for creating pipes, tubes, and other components with rotational symmetry, leveraging the force of rotation to ensure uniform metal distribution and potentially reduced defects.

### Process

- Molten metal is introduced into a rotating metal, or graphite mould, and held against the mould wall by centrifugal force until it solidifies

- A mould is set up and rotated along a vertical axis (reasonable rpm), or horizontal axis (200–1000 rpm is reasonable)

- The mould is coated with a refractory coating

- During cooling, lower density impurities will tend to rise towards the center of rotation

Figure: Centrifugal casting setup

# Lecture 7 – Investment Casting

## Investment Casting

Investment casting requires the use of a metal die, wax, ceramic slurry, furnace, molten metal, and any machines needed for sandblasting, cutting, or grinding. Investment casting, also known as lost-wax casting, is a versatile manufacturing process used across numerous industries to create intricate, high-precision parts. It is particularly well-suited for applications requiring complex geometries, tight tolerances, and smooth surface finishes.

Figure: Investment casting process — pattern tree, shell-making, casting, finished part

## Process Steps

- Pattern creation: wax patterns are typically injection molded into a metal die and formed as one piece (sometimes special designs made); cores may be used to form any internal features on the pattern

- Mold creation: this "pattern tree" is dipped into a slurry of fine ceramic particles, coated with more coarse particles, and then dried to form a ceramic shell around the patterns and gating system; this process is repeated until the shell is thick enough to withstand the pressure of the molten metal it will encounter

- Lost wax: the shell is placed into an oven and the wax is melted out, leaving a hollow ceramic shell that acts as a one-piece mould — hence the name "lost wax" casting

- Pouring: the mould is preheated in a furnace to approximately 1000°C (1832°F) and the molten metal is poured from a ladle into the gating system of the mould, filling the mould cavity

- Cooling: after the mould has been filled, the molten metal is allowed to cool and solidify into the shape of the final casting; cooling time depends on the thickness of the part, thickness of the mould, and the material used

- Casting removal: after the molten metal has cooled, the mould can be broken and the casting removed; the ceramic mould is typically broken using water jets, but several other methods are also used; once removed, the parts are separated from the gating system by sawing, grinding, or cold breaking (using liquid nitrogen)

- Finishing: finishing operations such as grinding or sandblasting are often used to smooth the part at the gates; heat treatment is also sometimes used to harden the final part

## Shapes Achievable

- Thin-walled: Complex shapes

- Solid: Cylindrical

- Solid: Cubic

- Solid: Complex shapes

- Thin-walled: Cylindrical

- Thin-walled: Cubic

## Materials and Part Size

Part size (weight): 0.02 oz – 500 lb

Materials: Alloy Steel, Carbon Steel, Stainless Steel, Aluminum, Copper, Nickel, Cast Iron, Lead, Magnesium, Tin, Titanium, Zinc

# Lecture 8 – Welding: Concept and Classification

## Introduction to Welding

- Welding is a materials joining process in which two or more parts are coalesced at their contacting surfaces by suitable application of heat and/or pressure

- Some welding processes are accomplished only by heat, no pressure required; some require both heat and pressure; some require only pressure, with no external heat

- Some welding processes require filler material to facilitate coalescence

- The assembly of joined parts by welding is called a weldment

## Classification of Metal Joining Processes

Joining Processes are broadly divided into Mechanical Bonding and Atomic Bonding (Welding).

- Mechanical Bonding: includes Temporary Joining (screw/nut-bolt) and Permanent Joining; further includes Rivets, Stitches, Staples, Shrink Fit

- Atomic Bonding (Welding): divided into Solid State welding, Liquid State (Fusion) Welding, and Liquid/Solid welding

- Solid State welding: includes Cold Welding, Friction Welding, Diffusion Welding, Hot Forge Welding

- Liquid/Solid welding: includes Brazing, Soldering, and Adhesive Bonding

- Liquid State (Fusion) Welding: divided by energy source into Electrical Energy and Chemical Energy

- Fusion welding – Electrical Energy: SMAW (Shielded Metal Arc Welding), Induction Welding, Resistance Welding, GMAW (Gas Metal Arc Welding), LBW (Laser Beam Welding), EBW (Electron Beam Welding), GTAW (Gas Tungsten Arc Welding)

- Fusion welding – Chemical Energy: Gas Welding, Thermit Welding

- Resistance Welding sub-types: Spot, Seam, Projection, Flash Butt, Upset Butt

- Other processes noted: Cold Welding, Ultrasonic Welding, Pressure Welding, Explosive Welding

Figure: Classification of joining processes — mechanical bonding vs atomic bonding (welding)

Figure: Classification of liquid-state (fusion) welding by energy source

## Sources of Energy in Welding Processes

- Chemical energy: Gas welding, explosive welding, Thermit welding

- Mechanical energy: Friction welding, Ultrasonic welding

- Electrical energy: Arc welding, Resistance welding

- Radiation energy: Laser beam welding, Electron beam welding

## Zones at the Weld Area

- Fusion zone: consists of a mixture of filler metal and base metal that have completely melted; characterized by a high degree of homogeneity among the component metals melted during welding

- Weld interface zone: a narrow boundary that separates the fusion zone from the heat-affected zone; consists of a thin band of base metal that was melted or partially melted (localized melting within the grains) during welding but then immediately solidified before mixing with the metal in the fusion zone

- Heat-affected zone (HAZ): the metal in this zone has experienced temperatures below its melting point, yet high enough to cause microstructural changes in the solid metal

(Diagram order across the joint: Unaffected base metal zone → Heat-affected zone (HAZ) → Weld interface → Fusion zone)

Figure: Zones at the weld area

## Types of Welding Joints

There are five basic types of joints for bringing two parts together for joining:

- Butt joint: the parts lie in the same plane and are joined at their edges

- Corner joint: the parts form a right angle and are joined at the corner of the angle

- Lap joint: consists of two overlapping parts

- Tee joint: one part is perpendicular to the other in the approximate shape of the letter "T"

- Edge joint: the parts are parallel with at least one of their edges in common, and the joint is made at the common edge(s)

Figure: Types of welding joints — butt, lap, corner, tee, edge

## Welding Defects

Common welding defects: Slag Inclusion, Undercut, Porosity, Incomplete fusion, Weld overlap, Underfill, Weld Spatter, Incomplete weld penetration.

### Undercut

- Causes: high current, improper electrode angle, long arc length

- Elimination: appropriate current, training to operator

- Repair: use smaller electrode

### Slag Inclusion

- Causes: insufficient current, slow travel speed

- Elimination: proper current, appropriate travel speed

- Repair: removed by grinding

### Porosity

- Causes: release of trapped gases

- Elimination: cleaning of the surface and ends

- Repair: removed by grinding

### Incomplete Fusion

- Causes: low current, fast travel speed, short arc gap

- Elimination: appropriate current and travel speed

- Repair: remove and reweld

### Weld Overlap

- Causes: untrained operator, steep electrode angle, faster travel speed

- Elimination: appropriate welding technique

- Repair: removed by grinding

### Underfill

- Causes: faster travel speed, improper welding technique

- Elimination: use stripper beads before cover pass

- Repair: clean and fill by welding

### Weld Spatter

- Causes: high arc current, magnetic arc blow

- Elimination: reduce arc current, shorten arc length

- Repair: removed by grinding

### Incomplete Weld Penetration

- Causes: low current, fast travel speed, short arc length

- Elimination: appropriate current, travel speed, and electrode

- Repair: clean and reweld

## References (as given in lecture)

- Ghosh, A. & Mallik, A.K.; Joining processes, Manufacturing Science, Latest edition.

- https://fractory.com/heat-affected-zone-causes-effects-reduction/

- Kalpakjian, S & Schmid, S.; Manufacturing Processes for Engineering Materials, Latest edition.

# Lecture 9 – Gas Welding and Types of Flame

## Gas Welding Equipment

- Gas cylinders

- Hose pipes and valves

- Cylinder pressure gauge

- Outlet pressure gauge

- Pressure regulators

- Blow pipe or torch and spark lighter

- Welding screens & goggles

- Gloves and apron

- Wire brush, trolley, chipping hammer

Figure: Gas welding equipment

### Gas Cylinders

- Oxygen gas cylinder is painted black colour and acetylene cylinder in maroon or red colour. Oxygen is filled at pressure up to 2000 PSI

- Acetylene is kept dissolved in acetone in the maroon cylinder. For safety reasons, the acetylene cylinder should not be exposed to higher temperatures

- Both cylinders are made with different types of threads (left-hand and right-hand)

### Pressure Regulators

Each cylinder is fitted with a pressure regulator that maintains supply pressure at a constant value. Supply pressure can be controlled and maintained at different values as required.

### Pressure Gauges

A pressure gauge measures the pressure with respect to atmospheric pressure. Two pressure gauges are mounted on each cylinder — one for cylinder pressure and one for supply pressure.

### Hose Pipes & Control Valves

Hose pipes carry gases from their respective cylinders to the blow pipe. Colour codes of hose pipes are the same as the cylinders. Hose pipes are made of good quality rubber for long life. Each cylinder is fitted with valves to control the flow of oxygen and acetylene separately, to obtain the desired flame.

### Torch

- Gas welding torches are low-pressure torches; gas cutting torches are high-pressure torches

- Both gases are mixed in a chamber of the torch and then flow out through the nozzle and are burnt by a spark lighter

- Gas cutting torch has holes for flow of the mixture of gases at the periphery and a separate oxygen flow hole at the centre

## Oxy-Acetylene Gas Welding

In oxy-acetylene welding, heat is generated as a result of a chemical reaction. The primary combustion process occurs in the inner core of the flame and involves the following reaction:

2CO + H₂ + 1.5 O₂ → 2CO₂ + H₂O + Heat

This reaction consists of the further burning of both the hydrogen and the carbon monoxide, and produces about two-thirds of the total heat. The temperature developed in the flame is approximately 3300°C.

## Types of Gas Welding Flames

### Neutral Flame

When equal amounts of oxygen and acetylene are mixed and burnt at the outlet of the welding torch, a neutral flame is obtained. This type of flame is made of two sharply defined zones, i.e., an inner white flame cone and an outer envelope of blue colour.

### Carburizing Flame

Consists of three zones: the inner cone, an outer envelope (as in the neutral flame), and a middle zone surrounding the inner cone extended to the outer envelope. Its size increases with increased quantity of acetylene.

### Oxidizing Flame

Produced by an excess amount of oxygen in the mixture. The oxygen-to-acetylene ratio varies between 1.15 and 1.50. The inner cone is relatively shorter, and excess oxygen turns the flame to a light blue colour. It burns with a harsh sound.

Figure: Types of gas welding flames — neutral, oxidizing, carburizing (reducing)

## Gas Cutting

- Gas cutting or flame cutting is an exothermic oxidation of the steel being cut

- The material is preheated by an oxy-fuel gas flame around 900°C

- The gas cutting nozzle has an outer ring of holes through which the preheating gas mixture is delivered, and a central hole through which only oxygen gas flows

- The exothermic oxidation of steel forms a fluid slag of iron oxide, and the metal section is pierced. Molten metal is carried away from the cut by the oxygen stream, leaving a cut. Movement of the cutting torch across the workpiece cuts a continuous slot

- Usually, steel sections up to 300 mm thick are easily cut

Figure: Gas cutting torch and operation

## References (as given in lecture)

- Ghosh, A. & Mallik, A.K.; Joining processes, Manufacturing Science, Latest edition.

- https://www.sciencedirect.com/topics/engineering/gas-welding

- Kalpakjian, S & Schmid, S.; Manufacturing Processes for Engineering Materials, Latest edition.

# Lecture 10 – Electric Arc Welding: SMAW and Submerged Arc Welding

## Introduction to Arc Welding

Processes that fall under Arc Welding: SMAW, GTAW, GMAW, Submerged Arc Welding.

SMAW (Shielded Metal Arc Welding) is also known as Manual Arc Welding. It is simple, portable, and inexpensive; suitable for almost all kinds of materials; can be used in hard-to-access areas; and has low initial cost.

Figure: Arc welding equipment and process, and weld bead

## Arc Welding Equipment

- Welding machine / transformer (AC)

- Electrode holder

- Cables

- Chipping hammer

- Wire brush

- Flux coated electrode

- Welding shields

- Goggles

- Gloves

- Apron

### Power Supply

- Both AC and DC are used for welding

- AC machine is a transformer which converts the supply to low voltage and high current; AC is recommended for ferrous metal

- For AC welding, power is required at 80 to 110 volts and 50 to 300 amperes

- For DC welding, normally power is required at 8 to 25 volts and 50 amperes

### Polarity in DC Welding

- Straight Polarity: electrode is made the negative pole and workpiece is made the positive pole; two-thirds of the total heat is generated at the positive pole and only one-third at the negative pole

- Reversed Polarity: electrode is made the positive pole and workpiece is made the negative pole; polarity is decided according to the requirement of heat at either pole

## Arc Welding Electrodes

- Welding electrodes: consumable electrodes and non-consumable electrodes

- Consumable electrodes provide filler metal; they are of two types — coated and bare electrodes

- Bare electrodes are used in case of gas shielded welding

- Additional filler metal is required for non-consumable electrodes (e.g., GTAW)

### Coated Electrodes

- Electrode is coated with flux

- Common flux ingredients that help in slag formation: asbestos, mica, silica, fluorspar, titanium dioxide, magnesium oxide, calcium oxide, manganese oxide, alumina, ferrous oxide, calcium fluoride, and silicates of potassium & sodium

- Some ingredients are used as per required properties in the weld

- Ingredients used to produce a reducing atmosphere: cellulose, dolomite, wood flour, starch

- Iron powder provides a higher deposition rate

- Manganese oxide, potassium silicate, and titanate are the alloying elements and stabilizers

### Merits of Flux on Electrodes

- Develops reducing atmosphere and prevents oxidation

- Forms separable slag from metal impurities

- Establishes arc stability

- Improves bead appearance

- Avoids weld spatter

- Provides necessary alloying elements to the weld pool

### Types of Flux Coating

- Cellulose coating: good penetration; CO and hydrogen generated during the process make the joint brittle

- Rutile coating: more titanium dioxide compared to cellulose coating

- Iron oxide coating: less gas produced, protection by slag

- Basic or low-hydrogen generating content coating: calcium carbonate and calcium fluoride produce CO + CO2; a short arc length is maintained for protection

## Other Welding Equipment

- Connecting Cables: used to connect electrode holder with the power source; flexible enough to facilitate easy movement of the electrode; provided with good insulation coating and can bear high current

- Welding Shield: used for protection of the welder's eyes from ultraviolet radiation, which may cause permanent damage to eyes

- Chipping Hammer: used to remove slag coating and clean the joint

## Arc Welding Control Parameters

- Work angle

- Travel angle

- Arc length

- Travel speed

## Submerged Arc Welding (SAW)

- Flux contains calcium oxide, calcium fluoride, and silica sintered to form coarse powder

- Flux powder is spread on the joint to be welded

- Metal electrode is fed into this flux

- Flux melts and covers the weld bead

- AC and DC are used, with current rating 200 to 2000 amps

- Used to weld thick sheets

Figure: Schematic diagram of Submerged Arc Welding

## References (as given in lecture)

- Ghosh, A. & Mallik, A.K.; Joining processes, Manufacturing Science, Latest edition.

- Lecture 19: https://drive.google.com/file/d/16o4wOavcwCZW9tFDZPvAkRmMzdt_NfeQ/view

- Kalpakjian, S & Schmid, S.; Manufacturing Processes for Engineering Materials, Latest edition.

- Lecture 14 & 15: https://nptel.ac.in/courses/112/107/112107089/

# Lecture 11 – Resistance Welding

## Principle of Resistance Welding

The heat is generated because of electric resistance. Heat is generated when current flows through resistance. The generated heat depends on the material's resistance, applied current, surface conditions, and the applied time period of current. Variants of resistance welding such as spot, seam, projection, flash butt, and upset butt work on this same principle. Pressure is also applied.

## Resistance Welding Equipment – Principal Elements

- Welding transformer, electrical circuits connected with electrodes, and current regulator

- A mechanical system consisting of a machine structure and mechanisms to hold the electrode and apply the welding pressure

- Control equipment to control the current magnitude and time

Figure: Resistance welding equipment (spot welding example)

## Seam Welding Process

- Disk-type electrodes are used

- Produces continuous type of welding between two sheets

- Disks are made of copper, and current is applied through them

- Current is applied in pulse form at time intervals

- Disks rotate continuously so that the metal sheets move forward

- Used to manufacture seam-welded pipes

## Projection Welding Process

- It is a modification of spot welding; one sheet is provided with projections and the other is plain — the projections are circular in form

- Projection diameter is equal to the thickness of the plate

- Sheets to be welded are kept between electrodes made of copper

- Current and pressure get concentrated at the projection areas during the process

- Pressure is applied by the upper movable electrode; the lower electrode is fixed

- By passing current, the projections get melted and welding is done

## Flash Butt Welding Process

- Normally used for butt joints; the two surfaces to be joined are brought into contact or near contact, and electric current is applied to heat the surfaces to the melting point, after which the surfaces are forced together to form the weld

- In addition to resistance heating, some arcing occurs (called flashing, hence the name flash welding) between the faying surfaces, so flash welding is sometimes classified in the arc welding group

- Current is usually stopped during upsetting

Figure: Flash butt welding — (1) heating by electrical resistance, (2) upsetting

## Upset Butt Welding Process

- Upset welding (UW) is similar to flash welding, except that in UW the faying surfaces are pressed together during heating and upsetting

- In flash welding, the heating and pressing steps are separated during the cycle

- Heating in UW is accomplished entirely by electrical resistance at the contacting surfaces; no arcing occurs

- When the faying surfaces have been heated to a suitable temperature below the melting point, the force pressing the parts together is increased to cause upsetting and coalescence in the contact region

- Thus, upset welding is not a fusion-welding process in the same sense as the other welding processes discussed

## References (as given in lecture)

- Ghosh, A. & Mallik, A.K.; Joining processes, Manufacturing Science, Latest edition.

- http://mewelding.com/resistance-welding-equipment/

- Kalpakjian, S & Schmid, S.; Manufacturing Processes for Engineering Materials, Latest edition.

# Lecture 12 – Soldering and Brazing

## Soldering

Soldering is a method of uniting two thin metal pieces using a dissimilar metal or an alloy by the application of heat.

### Soldering Equipment

- Soldering Iron / Station: the heart of the operation, providing the heat to melt the solder; soldering stations offer temperature control and can be more versatile

- Solder Wire: the fusible metal alloy that creates the bond

- Soldering Iron Stand: a safe place to rest the hot soldering iron when not in use

- Wet Sponge: used to clean the soldering iron tip of excess solder and oxidation

- Desoldering Tools: tools like desoldering wick or a solder sucker help remove excess solder or correct mistakes

### Soldering Types

- Soft solder: alloy of lead (37%) and tin (63%); melting temperature 150–350°C

- Hard solder: alloy of copper, tin, and silver; soldering temperature 600–900°C; used for stronger joints

- Flux: zinc chloride; cleans the joint surfaces and prevents oxidation

### Soldering Process

- 1. Preparation: clean the surfaces (free from oil, dirt, or oxidation, using a solvent, fine sandpaper, or steel wool); position the components in their correct positions

- 2. Apply Flux: apply a flux pen or paste to the joint area; flux removes remaining oxide layers and prevents new ones from forming during heating, ensuring the solder flows properly and creates a good connection

- 3. Heat the Joint: heat the joint, not the solder — touch the heated tip of the soldering iron to the surfaces to be joined for a few seconds to bring them to soldering temperature, so they can melt the solder

- 4. Apply Solder: while the joint remains hot, bring the solder wire into contact with the heated joint; the heat from the joint melts the solder (not the iron); the molten solder flows into the joint, forming a strong bond

- 5. Finish the Joint: remove the iron and solder wire and allow the joint to cool and solidify; once cooled, clean any remaining flux residue with a damp sponge or cotton swab

## Brazing

Brazing is a method of joining two similar or dissimilar metals using a special fusible alloy. Brazing temperature is the range above the solidus temperature (where the filler metal begins to melt) and below the melting points of the base metals being joined. Generally, this ranges from approximately 450°C (842°F) to 1200°C (2192°F).

### Brazing Heat Sources (Types of Brazing)

- Torch Brazing: uses a torch, often oxy-acetylene or propane, to heat the joint

- Induction Brazing: employs an induction coil to generate heat in the workpieces

- Furnace Brazing: involves placing the assembly in a furnace to heat it evenly

- Resistance Brazing: utilizes electrical resistance to create heat at the joint

### Brazing Equipment

- Brazing Torch: a handheld tool for torch brazing

- Brazing Machine: used in induction or resistance brazing processes

- Nozzle Set: assorted nozzles for torches to control the flame

- Lighter / Spark Lighter: for igniting torches

- Gas Regulators & Hoses: for controlling gas flow in an oxy-acetylene setup

- Personal Protective Equipment (PPE): Brazing Goggles (protect eyes from sparks and fumes), Welding Gloves (shield hands from heat and sparks), Protective Clothing (e.g., leather aprons)

### Brazing Process

- 1. Cleaning: thoroughly clean the components to remove oxides, grease, and other contaminants, as they can cause weak or brittle joints

- 2. Joint Design: create a joint with a precise, small gap (typically 0.05–0.2 mm) to facilitate capillary action for the filler metal

- 3. Fluxing: apply flux to prevent oxidation during heating and to promote wetting, allowing the filler metal to spread evenly

- 4. Heating: heat the assembled parts to a temperature just above the filler metal's melting point but below the melting point of the base metals

- 5. Applying Filler Metal: introduce the filler metal into the joint; it will melt and be drawn into the gap between the base metals by capillary action

- 6. Cooling: allow the assembly to cool, which solidifies the filler metal and creates a permanent, metallurgical bond

- 7. Post-Brazing: clean any remaining flux residue from the joint

## Distinguish Between Brazing and Soldering

| Brazing | Soldering |
| --- | --- |
| Melting point of the filler material is above 450°C | Melting point of the filler material is below 450°C |
| Dissimilar metals can be joined easily | Preferably similar metals can be joined |
| Good surface finish | Does not yield a good surface finish |
| Stronger joints | Less stronger joints |

## Comparison of Soldering, Brazing and Welding

| Soldering, Brazing | Welding |
| --- | --- |
| No direct melting of the base metals being joined | Direct melting of the base metals being joined |
| Useful for joining similar & dissimilar metals | Useful for joining similar metals |
| Brazing alloy and the solder have low melting points than the metals to be joined | Welding alloy has high melting point than the metals to be joined |
| Filler materials are solder and brazing alloy | Welding rod is used as filler material |

## References (as given in lecture)

- Ghosh, A. & Mallik, A.K.; Joining processes, Manufacturing Science, Latest edition.

- http://mewelding.com/resistance-welding-equipment/

- Kalpakjian, S & Schmid, S.; Manufacturing Processes for Engineering Materials, Latest edition.