## Slide 1
Casting Methods: Die Casting
Centrifugal Casting
Lecture 6

## Slide 2
Good for low temperature (approx. 650°C)
Faster than cold chamber machines
Cycle times must be short to minimize metal contamination
Metal starts in a heated cylinder
A piston forces metal into the die
The piston retracts, and draws metal in
Metal: Lead, Tin, Zinc
Hot Chamber die casting

## Slide 3
Hot Chamber die casting

## Slide 4
Hot Chamber die casting

## Slide 5
Casts high melting point metals ( > 700°C)
High pressures used
Metal is heated in a separate crucible
Metal is ladled into a cold chamber
The metal is rapidly forced into the mold before it cools
Copper, Brass and Aluminum can cast.
Cold Chamber die casting

## Slide 6
Cold Chamber die casting

## Slide 7
Extremely smooth surfaces (1 µm)
Excellent dimensional accuracy
Rapid production rate
Better mechanical properties compared to sand casting
Intricate parts possible
Cold Chamber die casting

## Slide 8
Summary Table for Hot and Cold Chamber die casting

## Slide 9
High initial die cost
Limited to high‐fluidity nonferrous metals
Part size is limited
Porosity may be a problem
Some scrap in sprues, runners, and flash, but this can be directly recycled
Die casting

## Slide 10
Applications
Carburetors
Automotive parts
Bathroom fixtures
Toys
Common metals
Alloys of aluminum, zinc, magnesium, and lead Also possible with alloys of copper and tin.
Die casting

## Slide 11
Centrifugal casting is a metal casting process that utilizes centrifugal force to distribute molten metal into a rotating mold, producing cylindrical or symmetrical parts. This method is particularly effective for creating pipes, tubes, and other components with rotational symmetry, leveraging the force of rotation to ensure uniform metal distribution and potentially reduced defects.
Centrifugal casting

## Slide 12
Centrifugal casting

## Slide 13
Process:
Molten metal is introduced into a rotating metal die,
metal, or graphite mould, and held against the mould wall by centrifugal force until it is solidified
A mold is set up and rotated along a vertical (rpm is reasonable), or horizontal (200‐1000 rpm is reasonable) axis.
The mold is coated with a refractory coating.
During cooling lower density impurities will tend to rise towards the center of rotation.
Centrifugal casting

## Slide 14
Centrifugal casting

## Slide 15
Centrifugal casting